™

# PRODUCT NAME

Shur-Cure

Clear & White

# MANUFACTURER

Paul M Wolff Co

460 N. Geneva Road

Lindon, UT 84042-1119

# PRODUCT DESCRIPTION

Shur-Cure is a VOC-compliant, ready-to-use, non-residual concrete curing agent for hardening and dustproofing interior and exterior surfaces. It can be easily applied to both horizontal and vertical surfaces as it deeply penetrates concrete surfaces to cure the concrete from within.  Shur-Cure is a water-based, clear sprayable liquid that offers residue free performance to which subsequent toppings, concrete, terrazzo, tiles, paints, epoxies or other toppings will satisfactorily bond and sealers, chemical hardeners and water repellents will penetrate.  Shur-Cure will not discolor and does not produce objectionable odors.  It is suitable for use in enclosed, well-vented areas where odor-free products are essential. Shur-Cure is recommended for areas where non-residual performance is critical and later toppings and sealers are desirable and scheduled.

## TECHNICAL DATA

Applicable Standards:

USDA approved

VOC compliant

Epoxy Coating Manufacturers

Asphalt & Vinyl Asbestos Tile Institute

Note: For ASTM-C309 membrane compliance, see other Paul M. Wolff Co. curing compounds and cure/sealers.

Coverage:

Surface porosity determines coverage rate.  Texture and absorption characteristics of the surface will dictate coverage rates.

Approximate Coverage:

Ft²/Gallon  m²/Liter

Broom Finish	200 - 300	    5 - 7.4

Trowel Finish	300 – 400	    7.4 – 9.8

Vertical Surfaces	200 – 300	    5 – 7.4

Old Surfaces	200 – 300	    5 – 7.4

## INSTALLATION

Apply to fresh concrete surfaces after final troweling when surface water glaze has disappeared and only when temperatures are above 40°F (4°C).  Apply only to frost-free surfaces.  Uniformly apply directly to the concrete surfaces by low pressure spray, soft bristle broom, brush, squeegee or roller at the rate specified.  Do not apply over standing water.  Do not puddle.  Do not over apply.

On old concrete floors, clean and restore surface as necessary.  Remove all oil and grease, paint and coatings to assure penetration and hardening.

Shur-Cure may not be ideal for application in clam, unvented, cool, or highly-humid conditions.  The application of Shur-Cure in cool, high humidity conditions prevents its proper penetration into the concrete surface, and hard to remove, unsightly white stains will result.  If these conditions exist, test and be prepared to immediately wash off and squeegee excess cure if it has not dried within four hours.

Drying Time:

Approximately 1 – 4 hours at 70°F (21°C).  Allow to dry 24 hours before opening to heavy traffic.

Clean Up:

Clean tools and equipment immediately after use, with fresh water.  If product dries, clean thoroughly with mineral spirits.

Limitations:

Not for use on colored concrete surfaces.  Protect adjacent surfaces – will stain and/or etch glass, metal and other trim.  Clean immediately with water.  Remove excess material and puddles from surface after application is complete.

Precautions:

Keep out of reach from children.  Wear protective clothing, gloves, shoes, and goggles.  Use with adequate ventilation in enclosed areas to facilitate proper drying.  Wash immediately from glass or metal surfaces and other overspray may damage.  Keep from freezing to prevent crystallization and settling.  Do not take internally. DO NOT induce vomiting.  If splashed in the eyes, flush thoroughly

with clean water for a minimum of 15 minutes.  May cause irritation to skin.  If brought into contact with the skin, wash thoroughly with soap and water.  Reseal container after each use.

CAUTION! Please refer to Product Material Safety Data Sheet (MSDS) before using product.

Packaging:

5 U.S. gal. (19L) container

55 U.S. gal. (208L) drums

## STORAGE/SELF LIFE

Shur-Cure containers are to be kept tightly sealed.  Keep from freezing. Store above 40°F (4°C). Shelf life is a minimum of 1 year in factory-sealed containers when stored properly.

## LIMITED WARRANTY

Manufacturer warrants that the Chemical Products sold to Purchaser will be of good quality and will conform to our published specifications in force on date of acceptance of the order or Manufacturer will replace or, at our election, refund the purchase price of any Product proved defective.  Any claim regarding Product defect must be received in writing within one year of the date of shipment.  Descriptions, representations and other information concerning Manufacturer’s Products contained in manufacturer’s catalogs, advertisements or other promotional materials or statements or representations made by Manufacturer’s sales agents or representatives shall not be binding upon Manufacturer and shall not be part of this limited warranty unless expressly identified in writing as Product Data Sheets and/or Application Manuals.  Purchaser shall determine the suitability of the Product for his intended use and Purchaser assumes all liabilities and risks whatsoever.  This limited warranty is Purchaser’s exclusive remedy.  MANUFACTURER SHALL NOT IN ANY EVENT BE LIABLE FOR INCIDENTAL OR CONSEQUENTIAL DAMAGES OF ANY NATURE WHATSOEVER, INCLUDING LOST PROFITS.  NO OTHER EXPRESS AND NO IMPLIED WARRANTIES OF ANY TYPE, WHETHER FOR MERCHANTABILITY, FITNESS FOR A PARTICULAR USE, OR OTHERWISE SHALL APPLY TO THE PRODUCTS.